**PAPER**

BOND PAPER

(link this to the inkjet bond paper page)

TRISOLVE POSTER PAPER

A multi-coated, weatherproof poster paper with high wet-strength and a glossy satin finish. This poster paper impresses with high colour brilliance and very good image definition. The material dries quickly even with high ink densities and does not cockle easily. Available in Thickness: 135gsm, 200gsm.

Finish: Satin.

Available sizes: 914mm, 1270mm, 1370mm, 1524mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

TEAR-RESISTANT SYNTHETIC PAPER

A synthetic tear-proof paper used for poster printing, point of sale, pull-up banners, scrolling banners. Scratch and smudge resistant.

Thickness: 135gsm.

Finish: Satin.

Available sizes: 1270mm, 1524mm.

Length: 30m.

Printer compatibility:.

PHOTO PAPER

A very high quality synthetic paper used for photographic reproduction. Scratch and smudge resistant.

Thickness: 220gsm.

Finish: Matt and Gloss.

Available sizes: 914mm, 1270mm, 1524mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

MAGNETIC PAPER (PROMO STEEL):

Promo Steel is a digital printable paper with an iron/ferrous coating that can be applied directly to magnetic substrates. This product is used for retail advertising, allowing you to replace the graphic with ease.

Thickness: gsm.

Finish: satin.

Available sizes: 1270mm.

Length: 30m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

**VINYL**

HAUS MONOMERIC VINYL (ONE YEAR)

A shorter term calendared white self-adhesive vinyl with a shrinkability factor of up to 8mm per metre. Used for stickers and general short term indoor and outdoor signage.

Thickness: 80 Micron.

Finish: Matt white, Gloss white.

Available sizes: 1370mm, 1524mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

HAUS MONOMERIC VINYL (THREE YEAR)

A short to medium term calendared self-adhesive vinyl with a shrinkability factor of up to 4mm per metre. Used for stickers and general indoor and outdoor signage.

Thickness: 100 Micron.

Finish: Matt white, Matt grey-back, Gloss white, Gloss grey-back, Matt clear, Gloss clear.

Available sizes: 1370mm, 1524mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

ORAJET 3164 MONOMERIC VINYL (4 YEAR)

A short to medium term calendared self-adhesive vinyl with a shrinkability factor of up to 4mm per metre. Used for stickers and general indoor and outdoor signage. Highly recommended for outdoor signage.

Thickness: 100 Micron.

Finish: Matt white, Matt grey-back, Gloss white, Gloss grey-back, Matt clear, Gloss clear.

Available sizes: 1370mm, 1600mm, 2000mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

HAUS HIGH-TACK VINYL

A short to medium term calendared self-adhesive vinyl with a high-tack adhesive to adhere to low energy surfaces which standard vinyls do not adhere to. These surfaces include rubber and plastic, such as bumpers and black dustbins. This vinyl has a shrinkability factor of up to 4mm per metre.

Thickness: 100 Micron.

Finish: Matt white.

Available sizes: 1370mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

HAUS PERFORATED VINYL

A white perforated vinyl with a black adhesive, designed for standard window, vehicle window and other glass applications. The black adhesive blocks the sun, while the small holes allows you to see out, while others viewing the graphic cannot see in.

Thickness: 140 Micron.

Finish: Matt black-back.

Available sizes: 1370mm, 1524mm.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

HAUS FROSTED VINYL

This self-adhesive vinyl gives a frosted sandblast effect to windows. Also known as etch glass or sandblast vinyl, it can be applied to windows and glass doors, even shower doors, allowing you to decide which area of the window you can see through and which area of the window is hidden.

Thickness: 80 Micron.

Available sizes: 1270mm, 1524mm.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

HAUS EEZIDOT VINYL

This unique white self-adhesive vinyl has an easydot adhesive technology, allowing you to apply the vinyl with ease. It is also repositionable and re-useable and leaves no glue residue behind when removed. Ideal for short to medium term window graphics in retail outlets.

Thickness: 120 Micron.

Finish: Matt.

Available sizes: 1370mm.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

HAUS REFLECTIVE VINYL (COMMERCIAL GRADE)

Reflective vinyl is similar to our standard vinyl in that it can be printed or cut to shape & applied to a surface. It is different in the fact that it has a metallic, reflective base that causes it to reflect back light when light is shone on it. Available in white (printable), as well as yellow, red, green, blue (non-printable).

Thickness: 0.11mm.

Finish: Gloss.

Available sizes: 1240mm.

Length: 45.7m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

AVERY REFLECTIVE VINYL (COMMERCIAL GRADE)

This film is a quality, enclosed lens retroreflective glass beaded material. Ideal for non-specification signage requirements such as off-road signage and parking lots. As an OmniDirectional beaded film, it provides confidence that all signs will perform with uniform visual reflectivity at all angles. Available in white (printable), as well as yellow, red, green, blue, brown (non-printable).

Thickness: 127 Micron.

Finish: Gloss.

Available sizes: 1240mm.

Length: 45.7m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

HAUS POLYMERIC VINYL (5 YEAR)

A medium term calendared self-adhesive vinyl with a shrinkability factor of up to 2mm per metre. Bubble-free adhesive. Used for general outdoor signage and stickers, as well as flat surface vehicle graphics.

Thickness: 60 Micron.

Finish: Gloss grey-back, Gloss clear.

Available sizes: 1370mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

ORAJET POLYMERIC VINYL 3165/3651RA (5 YEAR)

A medium term calendared self-adhesive vinyl with a shrinkability factor of up to 2mm per metre. Used for general outdoor signage and stickers, as well as flat surface vehicle graphics.

Thickness:

Orajet 3165 - 100 Micron.

Orajet 3651RA – 70 Micron (Rapid Air).

Finish: Gloss grey-back, Gloss clear.

Available sizes: 1370mm, 1600mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

AVERY WALL VINYL MPI2611

Avery Dennison MPI 2611 Wall Film is a tough, scuff-resistant, flexible, white premium calendered vinyl designed specifically for wall graphic applications. Easy installation and removable adhesive performance. Excellent fire rating.

Thickness: 152 Microns.

Finish: Matt.

Available sizes: 1370mm.

Length: 45.7m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

AVERY CAST VINYL MPI1105 (7-10 YEAR)

A long term cast self-adhesive vinyl with no shrinkage. Generally used for vehicle graphics but can be used for general indoor and outdoor signage as well as durable advertising, requiring clean removal after extended period of use. Ultra-conformable, excellent durability and conformability. Available with Easy Apply RS™ technology with the air-egress feature and maximum slideability and repositionability.

Thickness: 50 Micron.

Finish: Gloss grey-back.

Available sizes: 1370mm.

Length: 45.7m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

MACTAC CAST VINYL JT10700 (7 YEAR)

A long term cast self-adhesive vinyl with no shrinkage. Designed specifically for partial or total wrapping of vehicles and corrugated surfaces. Initial soft tack adhesive, bubble free, repositionable. Extreme conformability on 3D surfaces.

Thickness: 50 Micron.

Finish: Gloss grey-back.

Available sizes: 1370mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

**PVC**

BLOCKOUT PVC

A high-strength laminated flex (1000 x 1000 DIN) designed for outdoor use for billboards and banners. The black back gives 100% opacity so if the sun shines from behind, it does not interfere with the image printed on it.

Thickness: 510 gsm.

Finish: Matt.

Available sizes: 1370mm, 1600mm, 3200mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

ROLL-UP PVC (LAYFLAT)

A scrimless non-curl frontlit PVC banner ideally used for roll-ups and X-banners. The PVC has a scrimless smooth appearance.

Thickness: 510 gsm.

Finish: Satin.

Available sizes: 900mm, 1350mm, 1800mm, 2700mm, 3200mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

BACKLIT PVC

This backlit PVC is re-inforced and designed to be translucent so that when light shines through from behind, the design lights up. Generally used in lightboxes and backlit billboards that get viewed from a distance. Weather resistant with good light transmission.

Thickness: 500 gsm.

Finish: Satin.

Available sizes: 1370mm, 1600mm, 2500mm, 3200mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

MESH WITH LINER

A lightweight PVC mesh used for banners and other graphics applications and which allows air and sound to pass through. Ideal for high-wind applications. Can be used for building wraps, event graphics, fence banners and even indoor blinds as it is partially see-through.

Thickness: 270 gsm.

Finish: Matt.

Available sizes: 1370mm, 1600mm, 3200mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

**OTHER**

T-SHIRT TRANSFER VINYL (VIDEOFLEX)

A premium grade polyurethane vinyl which you can print and cut and then heat press onto t-shirts and then hot peel immediately. Suitable for cotton and polyester fabrics. Polyurethane vinyl is thinner and has more elasticity than PVC vinyls, therefore your t-shirt print will not crack. Excellent wash durability. This is a quality European vinyl.

Thickness: 90 Micron.

Finish: Matt.

Available sizes: 500mm, 1000mm.

Length: Various.

Printer compatibility: Solvent, Eco-solvent, Latex.

**FILMS**

BACKLIT FILM

Polyester backlit film is a translucent material on which graphics or text is printed so that when light shines through from behind, the design lights up. Generally used in lightboxes and windows.

Thickness: 200 Micron.

Finish: Matt, gloss.

Available sizes: 1370mm, 1524mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

SOLVENT POLYESTER CANVAS

A good quality, fire-retardant canvas comprising of a 65% polyester and 35% cotton blend. used to print photographic, art reproductions and lightboxes. Can be stretched over a frame without the edges cracking.

Thickness: 260gsm.

Finish: Matt.

Available sizes: 1370mm, 1524mm.

Length: 30m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

SOLVENT COTTON CANVAS

This exceptional quality pure cotton canvas has a transparent coating that eliminates the need for a sealant. Used to print photographic and art reproductions. Can be stretched over a frame without the edges cracking.

Thickness: 350gsm.

Finish: Satin.

Available sizes: 914mm, 1370mm, 1524mm.

Length: 18m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

PICASSO CANVAS

A high quality waterfast white canvas comprising of a 35% polyester and 65% cotton blend. For professional photographic and artistic reproductions. Excellent colour gamut with rich blacks.

Thickness: 370 gsm.

Finish: Satin.

Available sizes: 914mm, 1370mm, 1524mm.

Length: 15m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

MURAMOUR SABLE WALLPAPER

Muramour Sable is a paper-backed vinyl with a fine sand texture that is as subtle as it is alluring.  It has a warm white appearance. Very easy to install and repositionable during installation when handled with care. It is also washable and scratch resistant. The Muramour range carries the highest of fire-ratings which is essential for use in public spaces.

Thickness: 300 gsm.

Finish: Matt.

Available sizes: 1300mm.

Length: 30m, 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

MURASPEC GRAPHITE WALLPAPER

For a slightly cooler white, Muramour graphite will give you a brilliant colour gamut with a slightly rough sand texture. Very popular amongst applicators, this paper backed vinyl is easy to install and comes with the highest of fire ratings.

Thickness: 300 gsm.

Finish: Matt.

Available sizes: 1300mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.

GVTEX SELF-ADHESIVE WALLPAPER

A self-adhesive laminated PVC with a very light sand texture ideally suited for application onto smoother walls.

Thickness: 300 gsm.

Finish: Satin.

Available sizes: 1370mm.

Length: 50m.

Printer compatibility: Solvent, Eco-solvent, Latex and UV.